| SBR 1500 | SBR 1712 | BR 1220 | Butyl Rubber IIR | Polychloroprene CR | Reclaim |
| --- | --- | --- | --- | --- | --- |
| Cold Butadiene Styrene Rubber | Cold Butadiene Styrene Rubber extended with 37.5 parts of highly aromatic oil | Or Equivalent Cis- 1:4 Poly Butadiene rubber, Polymerized | Copolymer of isobutylene and isoprene | Polychloroprene rubber, regulated by mercaptan with little tendency to crystallization | Reclaim Rubber (Superfine grade) from tyres with high content of natural rubber. |
| Bonded Styrene % 22-25 | Bonded Styrene % 22-25 | NON STAINING | Unsaturation Mol. % or Double Bond 1.4-2 |  | Form: Black Sheets |
| Volatile Matter Max. % 0.75 | Volatile Matter Max. % 0.75 | Volatile Matter Max. % 0.75 | Volatile Matter Max. % 0.3 | Volatile Matter Max. % 0.5 | Acetone Extract % 10-30 |
| Ash Content Max. % 1.50 | Ash content Max % 1.50 | Ash content Max % 0.5 | Ash content Max % 0.5 | Ash content Max % 1 | Ash Content % 10-30 |
| Organic Acid % 4.5-7.25 | Organic Acid % 3.5-6.5 | Content of Cis-1.4 Structure Mol. % Min. 95 |  | Specific Gravity g/cm³ 1.23±0.1 |  |
| Viscosity Moony/ 100Cº (1+4) ML 44-60 | Viscosity Moony/ 100Cº (1+4) ML 40-60 | Viscosity Moony/ 100Cº (1+4) ML 38-50 | Viscosity Moony/ 125Cº (1+8) ML 46-56 | Viscosity Moony/ 100Cº (1+4) ML 36-46 without treatment | Viscosity Moony/ 100Cº (1+4) ML 30-80 |
| Packing: Each bale should be wrapped in polyethylene film. An Assembly of bales to be packed in a plastic film. The pallets should be wooden boxes. | Packing: Each bale should be wrapped in polyethylene film. An Assembly of bales to be packed in a plastic film. The pallets should be wooden boxes. | Packing: Each bale should be wrapped in polyethylene film. An Assembly of bales to be packed in a plastic film. The pallets should be wooden boxes. | Packing: Each bale should be wrapped in polyethylene film. An Assembly of bales to be packed in a plastic film. The pallets should be wooden boxes. | Packing: Paper or plastic bags (polyethlenelined) on pallets | Sheets packed in plastic film, on pallet. The pallets should be wooden boxes. |