HLA Chemicals Pvt. Ltd.

71/A, Krishna House, S.T. Bus Stand Road,

Ganeshpeth,

NAGPUR – 440018,

Maharashtra,

INDIA.

| Tel. | : | 91 | - | 712 | - | 2601225 |
| --- | --- | --- | --- | --- | --- | --- |
| Fax | : | 91 | - | 712 | - | 2723789 |
| E-mail | : | brijeshagrawal1979@yahoo.co.in |  |  |  |  |

SPECIFICATIONS

Chemical Composition of Dry Fly Ash

| Sl.No. | Type of chemicals | In % |
| --- | --- | --- |
| 1 | Silica | 43.20 |
| 2 | Alumina | 23.89 |
| 3 | Iron Oxide | 18.36 |
| 4 | Calcium Oxide | 9.80 |
| 5 | Magnesium Oxide | 4.20 |
| 6 | Sodium oxide | - |
| 7 | Sulphur Trioxide | Trace |
| 8 | Phosphorus pentaoxide | 0.05 |
| 9 | Potassium oxide | - |
| 10 | Loss on ignition | 0.50 |

Physical Properties

| Sl.No. | Description | Property |
| --- | --- | --- |
| 1 | Colour | Grayish white powder |
| 2 | Bulk Density | 1047 Kg/M3 |
| 3 | Specific Gravity | 2.2 |
| 4 | Fineness | 325 µ M-20 µ M |
| 5 | Moisture | Less Than 0.3% |

Particle Size of Fly Ash (In %)

| Sl.No. | Size in MM | In % |
| --- | --- | --- |
| 1 | 0.6 to 0.3 mm | 0.4 % |
| 2 | 0.3 to 0.15 mm | 2.42 % |
| 3 | 0.15 to 0.75 mm | 6.20 % |
| 4 | Less than 0.075 mm | 90.98 % |
| 5 | Specific Gravity | 1.89 % |