Technical Specifications for shaft rollers

1 - Application:

The shaft rollers are requested for 2 X 1500 ton clinker dry process, of the following technical datas:

- Tube diameter			4.6m

- Length				75 m

- Slope				3.5 %

- Bearings, group number		3

- Efficiency 1500 t.cl/day; with the possibility of increasing it up to 2000 t/day.

- Weight of each kiln during operation; 1500t. approx.

2 - The required quantity:

- ( 8 ) shaft rollers, according to the attached drawing No. 0510 (Rollers with shaft Assembly).

- ( 4 ) Pieces left housing bearings, as per drawing no E03/50 (DVE 4272.06.01.00)

- ( 4 ) Pieces right housing bearings, as per drawing NO. E03/51 (DVE 4272.06.03.00)

Note: for your reference, we enclose draw .No. E03/49.

- ( 20 ) pieces bronze bearing, as per draw. No.E03/45 (DVE 4272.06.01.03.00/A)

3 - The materials:

(8) complete shaft rollers consisting of:

1. Rollers diameter: 1700 X 1050, as per drawing No. 0510/2 the requested material is GS60 -3 , according to DiN .stand .NO.1. 0558.

2. Shaft's diameter: 750 X 2920, as per design drawing no. 0510/1 the material is CK60, according to DIN. STAND. NO. (1.1221).

3. Pieces shrinking rings: as per of draw. No. 0510 /3.the material is CK60, according to DIN. stand. N0. (1. 1221).

4. The supplier could offer also an alternative metals, which their quality should be better than the required, mentioning the reference standards and all the technical datas, such as chemical composition & physical properties.

5. The supplier should submit the detailed and total weights of the shaft rollers; and should point-out to the technical reasons for these weights (increase / decrease), bearing in mind that the weight of the old roller, which was delivered by the Romanian side is ( 20 ) t/each.

6.  The supplier should define the warranty operational period of the offered rollers.

7. The supplier should have to know that the shafts will be technically fitted with the bearings via (interference fitting).

8. The supplier should establish the type of metal of all delivered pieces in the right & left housing bearings and of the bronze metal (EO3/49).

9. The supplier could submit an alternative offer to be suited with the existing situation (for right & left housing bearings, EO3 /50; EO3 / 51)

10. If you have lubrication on system better than ours, please offer it.

4 - The quality control:

- The shaft rollers should be free of cavities, inclusions, sands pores or crack.

- All burrs projections, .....etc. should be removed.

- Repaired rollers are not acceptable.

- The required shaft rollers should be ready for mounting without any modifications.

5 - Documentations:

The supplier should submit all catalogues of maintenance and mounting instructions

Remark:

Please find here below a sketch showing the distance between the three supports – rollers of the kiln.